Supplementary material

Table S1. Composition of the precursor solution used for synthesis.

| Sample name | Ethylene glycol volume (ml) | Weight of zinc acetate dihydrate (g) | Weight of silver acetate anhydrous (g) | Final water content of the precursor solution (weight percentage) |
| --- | --- | --- | --- | --- |
| ZnO NPs 1.5% H2O [1] | 525 | 35 g | 0 | 1.5 |
| ZnO NPs 6% H2O |  |  |  | 6 |
| ZnO+0.1%Ag NPs 1.5% H2O |  |  | 0.0266 | 1.5 |
| ZnO+0.1%Ag NPs 6% H2O |  |  | 0.0266 | 6 |
| ZnO+1%Ag NPs 1.5% H2O [1] |  |  | 0.2689 | 1.5 |
| ZnO+1%Ag NPs 6% H2O |  |  | 0.2689 | 6 |

Table S2. Characteristics of samples.

| Sample name | Skeleton density, ρs±σ (g·cm-3) | Specific surface area, as (m2·g-1) | Average particle size from SSA BET, d±σ (nm) | Average crystallite size, Scherrer equation, d±σ (nm) |
| --- | --- | --- | --- | --- |
| ZnO SMPs [2] | 5.59 ± 0.03 | 4.5 | 240 ± 30 | 124 ± 11 |
| ZnO NPs 1.5% H2O [1] | 5.09 ± 0.06 | 48.4 | 25 ± 2 | 31 ± 8 |
| ZnO NPs 6% H2O | 5.38 ± 0.05 | 17.2 | 65 ± 6 | 40 ± 10 |
| ZnO+0.1%Ag NPs 1.5% H2O | 5.16 ± 0.07 | 40.0 | 29 ± 2 | 17 ± 5 (ZnO) 31 ± 10 (Ag) |
| ZnO+0.1%Ag NPs 6% H2O | 5.37 ± 0.06 | 14.2 | 79 ± 2 | 39 ± 12 (ZnO) 31 ± 10 (Ag) |
| ZnO+1%Ag NPs 1.5% H2O [1] | 5.05 ± 0.05 | 44.4 | 27 ± 2 | 22 ± 3 (ZnO) 45 ± 20 (Ag) |
| ZnO+1%Ag NPs 6% H2O | 5.31± 0.09 | 21.4 | 53 ± 2 | 35 ± 5 (ZnO) 31 ± 15 (Ag) |

Table S3. Results of the analysis of the chemical composition of samples. Energy-dispersive spectrometry (EDS) was used for the analysis.

| Sample name | Actual dopant content (mol%) |  | Nominal composition (mol%) |  | Weight content of ZnO and Ag in 100 mg of sample (mg) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Zinc | Silver | Zinc | Silver | ZnO | Ag |
| ZnO+0.1%Ag NPs 1.5% H2O | 99.91 ± 0.04 | 0.09 ± 0.04 | 99.9 | 0.1 | 99.881 | 0.119 |
| ZnO+0.1%Ag NPs 6% H2O | 99.85 ± 0.06 | 0.15 ± 0.06 | 99.9 | 0.1 | 99.801 | 0.199 |
| ZnO+1%Ag NPs 1.5% H2O [1] | 99.05 ± 0.20 | 0.95 ± 0.20 | 99.00 | 1.00 | 98.745 | 1.255 |
| ZnO+1%Ag NPs 6% H2O | 98.95 ± 0.20 | 1.05 ± 0.20 | 99.00 | 1.00 | 98.613 | 1.387 |

Table S4. Results of multivariate analysis of variance (MANOVA) for the number of leaves, shoot and root system fresh and dry weights of Chrysanthemum × morifolium plantlets, depending on the cultivar and experimental treatment.

| Source of variation | Wilks’ lambda value | d.f. | F | p |
| --- | --- | --- | --- | --- |
| Cultivar | 0.4440 | 1 | 56.6 | 0.000 |
| Treatment | 0.2799 | 22 | 3.0 | 0.000 |
| Cultivar × Treatment | 0.3819 | 22 | 2.2 | 0.000 |

Table S5. Results of multivariate analysis of variance (MANOVA) for the leaf architecture parameters of Chrysanthemum × morifolium plantlets, depending on the cultivar and experimental treatment.

| Source of variation | Wilks’ lambda value | d.f. | F | p |
| --- | --- | --- | --- | --- |
| Cultivar | 0.9734 | 1 | 3.91 | 0.004 |
| Treatment | 0.7422 | 22 | 2.02 | 0.000 |
| Cultivar × Treatment | 0.7476 | 22 | 1.97 | 0.000 |

Table S6. Results of multivariate analysis of variance (MANOVA) for the root system architecture parameters of Chrysanthemum × morifolium plantlets, depending on the cultivar and experimental treatment.

| Source of variation | Wilks’ lambda value | d.f. | F | p |
| --- | --- | --- | --- | --- |
| Cultivar | 0.5957 | 1 | 25.5 | 0.000 |
| Treatment | 0.1611 | 22 | 3.68 | 0.000 |
| Cultivar × Treatment | 0.4222 | 22 | 1.59 | 0.000 |